Western Europe – Western China International Transit Corridor Road reconstruction project

Lot-8 (1752 Km –1807 Km)

Length: 55 Km (2-Lane)

Contractor: "Akkord –Okan JV"
Engineer: LLP"Kazdorproject"
Amount of Contract: 15.881 billion tenge;
In 2010 - of 2013 Disbursement –15 686 115 785,83 tenge;

Subcontractors:

1.  “MO-1” LLP - Construction of Bridge across Shirkeili Channel at PK 623+87, L=89.5 m

2.”SK Stroymost 2010” LLP - Construction of Bridges at PK 680+83, PK 690+38, PK 712+70, PK 755+25, PK 900+30 and Overpass at PK 734+80

3. “Almatymostospetsstroi” LLP, construction of bridge No.1, PK 570+80.45  ‘Center Energo Service” LLP – Relocation of PTL-35kW, PK 714+20, PK 734+28, external lighting km 1806-1807 and interchange Shirkeilii village, “Feb-Stroy” LLP road signs and markings.

4. “KREK” JCS – transfer of PTL

Laboratory.     Missing sampling and core sample and their treatment, measurement and testing in accordance with the technical specifications of the Contract are processing for all kinds of work. The selection and control of concrete mix emission made by ACP and CMP and also quality control of procured materials are processing. Verification of pavement’s smoothness and testing of concrete samples are processing.

The laboratory is 95% equipped.

Status of works as of 30.12.2013

| No | Description | Total Contract | Achieved in 2010-2012 | Plan for 2013 | Actual in 2013 | Actual in percentage (%) | Delays |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Earth work, Thos. M3 | 2100,604 | 1474,89 | 395,4 | 395,4 | 100% | 0 |
| 2 | Sub base, km | 56,82 | 56,2 | 1 | 0,8 | 81% | 0,2 |
| 3 | Base course 20 cm, Km | 56,82 | 56,1 | 1,1 | 0,9 | 80% | 0,2 |
| 4 | Porous Asphalt, 12 cm, Km | 56,82 | 56,2 | 1 | 0,8 | 81% | 0,2 |
| 5 | Binder course 10 cm, Km | 56,82 | 56,0 | 1,2 | 1 | 81% | 0,2 |
| 6 | Wearing course, 5 cm, Km | 57,21 | 14,72 | 42,5 | 42,2 | 99% | 0,3 |
| 7 | Culverts, No. | 59 | 48,8 | 10,2 | 8,01 | 96% | 2,19 |
| 8 | Bridges No | 8 | 5,3 | 2,7 | 0,61 | 74% | 2,09 |

| Materials procurement | Plan for 2013 | Fact on 30.12.2013 | Performed % | Remaining. (+,-) |
| --- | --- | --- | --- | --- |
| 1 | Crushed stone thousand/ton | 236,4 | 236,4 | 100 | 0 |
| 2 | GSM thousand/ton | 124,2 | 124,2 | 100 | 0 |
| 3 | RCP thousand m3 | 1,46 | 1,5 | 100 | 0 |

Status of equipment for the execution of work program for 30.12.2013

| No | Name of equipment | Requirement | Actual | Additional required |
| --- | --- | --- | --- | --- |
| 1 | Dozer | 5 | 2 | 3 |
| 2 | Excavator | 11 | 5 | 6 |
| 3 | Loader | 17 | 4 | 13 |
| 4 | Rollers | 24 | 9 | 15 |
| 5 | Grader | 9 | 4 | 5 |
| 6 | Dumper | 98 | 62 | 36 |
| 7 | Paver | 2 | 2 | 0 |
| 8 | ACP | 1 | 1 | 0 |
| 9 | CCP | 1 | 1 | 0 |
| 10 | Crushing Plant | 1 | 1 | 0 |
| 11 | Others | 79 | 58 | 21 |
| Total: | 248 | 149 | 99 |